 CopperCraft, Inc.

Cupola Specifications

General

1.01 Description of work

A. Furnish and install complete CopperCraft Custom/Standard Cupolas (with attachment points for Lightning Protection System) and other accessories as required in accordance with CopperCraft specifications and plans and details.

B.
All sheet metal products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

Products

2.01 Manufacturer

CopperCraft, Inc.

4995 Keller Haslet Road

Keller, Texas 76244

1-800-486-2723

2.02 Materials

A.
Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than 16oz per square foot.

B.
Leadcoated Copper: ASTM Specification B101 (Type 1), Class A, weighing not less than 16oz per square foot.

C.
Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum.

D. Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium in a (preweathered, mill) finish and not less than .7mm thickness.

E.
Prefinished Aluminum: Sheet aluminum to be (.032, .040) aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM Specification B209. Finish to be Kynar 500 formulization in a standard color as selected by the Architect.

Execution

3.01 Inspection

All surfaces to which sheet metal is to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

All sheet metal work shall conform to standards set forth in the following publications.

1. Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual

2. Copper Development Association (C.D.A.) Copper Brass Bronze Design Handbook 

3. Revere Copper Products, Inc,; Copper and Common Sense

