CopperCraft, Inc.

Louver/Window Cupola Specifications

General

1.01 Description of Work

A. Furnish and install metal cupola(s) and accessories in accordance with CopperCraft Specifications and details.

B. All sheet metal Louver/Window Cupola products shall be manufactured by CopperCraft in sizes, styles, materials, and designated airflows as indicated below and shown on drawings.

1. Louvers to be shop fabricated brake formed with (soldered/sealed) watertight frame construction and to include a (insect, bird) screen of compatible material. [Cupola to include ¼” (clear)(tinted) tempered glazing as an integral part of cupola assembly.]

2. Louver to have a minimum free area of (    ) sq. in. to provide adequate ventilation of attic area.

3. [Cupola to include sub-frame of welded aluminum tube/plate, 3/8” CDX plywood sheathing, and flexible self-adhering rubberized membrane waterproofing.] 

Products

2.01 Manufacturer


CopperCraft, Inc.


404 East Dallas Road


Grapevine, TX  76051


PH 800-486-2723

2.02 Materials

A. Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than (16, 20, 24, 32) ounces per square foot.

B. Leadcoated Copper: ASTM Specification B101 (Type 1), Class A, weighing not less than (16, 20) ounces per square foot.

C. Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum steel.

D. Prefinished Aluminum: Sheet aluminum to be (.032, .040, .050) aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM Specification B209. Finish to be Kynar 500 formulization in a standard color as selected by the Architect.

E. Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium, either mill finish or preweathered, .027” (.7mm) minimum.

Execution

3.01 Inspection

All surfaces or openings to which Cupola is to be applied shall be smooth, sound, clean, plumb, dry, and free from defects that might affect the application.

3.02 Installation

A.
All sheet metal work shall conform to standards set forth in the following publications:

1. Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA)  Architectural Sheet Metal Manual.

2.
CDA Copper Design Manual, published by the Copper Development Association.

3. Copper and Common Sense – Sheet Copper Design Principles and Construction Techniques Manual, Published by Revere Copper Products

B.
Fasten cupola to roofing curb as designated on shop drawings and approved by the Architect.

