 CopperCraft, Inc.

Conductor Head Specifications

General

1.01 Description of work

A. Furnish and install complete CopperCraft Custom/Standard Conductor Heads and other accessories as required in accordance with CopperCraft specifications and plans and details.

B.
All sheet metal products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

1.01 Related Work

A. Gutter and Downspouts

B. Flashing & Trim

C. Accessories

Products

2.01 Manufacturer

CopperCraft, Inc.

4995 Keller Haslet Road

Keller, Texas 76244

1-800-486-2723

2.02 Materials

A.
Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than 16oz per square foot.

B.
Leadcoated Copper: ASTM Specification B101 (Type 1), Class A, weighing not less than 16oz per square foot.

C.
Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum.

D. Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium.

Execution

3.01 Inspection

All surfaces to which sheet metal is to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

All sheet metal work shall conform to standards set forth in the following publications.

1. Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual

2. Copper Development Association (C.D.A.) Copper Brass Bronze Design Handbook 

3. Revere Copper Products, Inc,; Copper and Common Sense

