 CopperCraft, Inc.

Downspout Specifications

General

1.01 Description of work

A. Furnish and install complete CopperCraft Downspout and Conductor Head system including hangers, outlets and elbows and other accessories as required in accordance with CopperCraft specifications and plans and details.

B.
All sheet metal products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

1. Downspouts to be 5” x 7” rectangular leaders, or as shown on drawings and be installed with CopperCraft downspout hangers and elbows. Mount downspouts with a minimum of two hangers per 10-foot section.

2. Conductor Heads or Collector Boxes shall be of size and style as indicated on the drawings and be of soldered or welded construction and post painted to match downspouts with a post applied Kynar 500 finish.

1.02 Related Work

A. Conductor Heads

B. Flashing & Trim

C. Accessories

Products

2.01 Manufacturer

CopperCraft by Fabral

404 E Dallas Rd
Grapevine, TX  76051
1-800-486-2723

2.02 Materials

A. Aluminum: Sheet aluminum to be .040 aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM B209.

B. Finish: Finish shall be Kynar 500 Fluorucarbon coating applied by operation of coil coating line with a top film thickness of 0.70 to 0.90 mil over 0.25 to 0.35 mil prime coat for a total dry film thickness of .95 to 1.25 mil. Bottom side shall be coated with a primer for a dry film thickness of .25 mil. Strippable coating shall be applied to the sheet to protect the finish during fabrication, shipping and field handling. REMOVE THE FILM either immediately before or immediately after installation. Do not allow the film to remain on the product when the product will be exposed to the weather.

Execution

3.01 Inspection

All surfaces to which sheet metal is to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

All sheet metal work shall conform to standards set forth in the following publications.

1. Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual

2. Copper Development Association (C.D.A.) Copper Brass Bronze Design Handbook 

3. Revere Copper Products, Inc,; Copper and Common Sense

