 CopperCraft, Inc.

Gutter and Downspout Specifications

General

1.01 Description of work

A. Furnish and install complete CopperCraft Gutter and Downspout System including endcaps, miters, hangers, outlets and elbows and other accessories as required in accordance with CopperCraft specifications and plans and details.

B.
All sheet metal products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

1. Gutters to be (4”, 5”, 6”, 7”, 8”) CopperCraft (Half Round, Ogee, K-style, Quarter Round, Rolled Box Bead, custom) gutter installed with CopperCraft (fascia-mount or roof-mount) gutter hangers & inside straps mounted at 30” on center. 

2. Downspouts to be CopperCraft (3”, 4”, 5”, 6”) (Round, Square, Rectangular, Twisted) downspout, or as shown on drawings and be installed with CopperCraft downspout hangers and elbows. Mount downspouts with a minimum of two straps per 10-foot section.

1.02 Related Work

A. Conductor Heads

B. Louvers and Louver Dormers

C. Finials and Spires

D. Flashing & Trim

E. Roof Panels

F. Accessories

Products

2.01 Manufacturer

CopperCraft by Fabral

404 E Dallas Rd

Grapevine, TX  76051

1-800-486-2723

2.02 Materials

A. Copper:
99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than 16 ounces per square foot.

B. Freedom Gray Copper (zinc/tin alloy coated copper): ASTM Specification B370, weighing not less than 16 ounces per square foot.

C. Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum steel.

D. Prefinished Aluminum: Sheet aluminum to be (.032, .040, .050) aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM Specification B209. Finish to be Kynar 500 formulization in a standard color as selected by the Architect.

E. Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium, either mill finish or pre-weathered, .027” (.7mm) minimum.

Execution

3.01 Inspection

All surfaces to which sheet metal is to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

All sheet metal work shall conform to standards set forth in the following publications.

1. Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual

2. Copper Development Association (C.D.A.) Copper Brass Bronze Design Handbook 

3. Revere Copper Products, Inc,; Copper and Common Sense

