CopperCraft, Inc.

Prefabricated Awning Specifications

# General

  - Description of Work

- Furnish and install metal awning and accessories in accordance with CopperCraft Specifications and details.

- All sheet metal awning products shall be manufactured by CopperCraft in sizes, styles, materials, as shown on drawings.

- Awning to include bottom plywood/copper panel to be installed after attaching awning to structure.

- Awning to include sub-frame of welded aluminum tube/plate, 3/8” plywood sheathing cladding, and flexible self-adhering rubberized membrane waterproofing.

- Roof panels to be 1” tall from 16oz copper sheet.

# Products

2.01 Manufacturer

CopperCraft, Inc.

404 East Dallas Road

Grapevine, TX  76051

PH 800-486-2723

2.02 Materials

- Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than 16 ounces per square foot.

- Leadcoated Copper: ASTM Specification B101 (Type 1), Class A, weighing not less than 16 ounces per square foot.

- Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum steel.

- Prefinished Aluminum: Sheet aluminum to be .032 aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM Specification B209. Finish to be Kynar 500 formulization in a standard color as selected by the Architect.

- Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium, either mill finish or preweathered, .027” (.7mm) minimum.

# Execution

3.01 Inspection

All surfaces or openings to which Awning is to be applied shall be smooth, sound, clean, plumb, dry, and free from defects that might affect the application.

3.02 Installation

A.	All sheet metal work shall conform to standards set forth in the following publications:

- Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA)  Architectural Sheet Metal Manual.

2.	CDA Copper Design Manual, published by the Copper Development Association.

- Copper and Common Sense – Sheet Copper Design Principles and Construction Techniques Manual, Published by Revere Copper Products

B.	Fasten awning to wall structure as designated on shop drawings and approved by the Architect/Engineer.