CopperCraft, Inc.

Louver Dormer Specifications

# General

  - Description of Work

- Furnish and install metal louver dormer(s) and accessories in accordance with CopperCraft Specifications and details.

- All sheet metal Louver Dormer products shall be manufactured by CopperCraft in sizes, styles, materials, and designated airflows as indicated below and shown on drawings.

- Louvers to be shop fabricated brake formed with (soldered) watertight frame construction and to include a (insect, bird) screen of compatible material. [Dormer to include ¼” (clear)(tinted) tempered glazing as an integral part of dormer assembly.]

- Dormer Louver to have a minimum free area of (    ) sq. in. to provide adequate ventilation of attic area.

- Dormer to include full 12” wide roof flange at sides and back of dormer to allow watertight installation.

- [Dormer to include sub-frame of welded aluminum tube, plywood cladding, and flexible self-adhering rubberized membrane waterproofing.] (as dictated by size – see frame requirement charts).

# Products

2.01 Manufacturer

CopperCraft, Inc.

4995 Keller Haslet Road

Keller, TX 76244

PH 800-486-2723

2.02 Materials

- Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than (16, 20, 24, 32) ounces per square foot.

- Freedom Gray Copper: ASTM B370, weighing not less than 16 ounces per square foot.

- Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum steel.

- Prefinished Aluminum: Sheet aluminum to be (.032, .040, .050) aluminum alloy 3003-H14 lock forming quality (LFQ) ASTM Specification B209. Finish to be Kynar 500 formulization in a standard color as selected by the Architect.

- Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium, either mill finish or preweathered, .027” (.7mm) minimum.

# Execution

3.01 Inspection

All surfaces or openings to which Dormer is to be applied shall be smooth, sound, clean, plumb, dry, and free from defects that might affect the application.

3.02 Installation

A.	All sheet metal work shall conform to standards set forth in the following publications:

- Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA)  Architectural Sheet Metal Manual.

2.	CDA Copper Design Manual, published by the Copper Development Association.

- Copper and Common Sense – Sheet Copper Design Principles and Construction Techniques Manual, Published by Revere Copper Products

B.	Fasten dormer to roof structure as designated on shop drawings and approved by the Architect.