CopperCraft, Inc.

Flat Seam Panel Specifications

# General

  - Description of work

- Furnish and install complete CopperCraft Flat Seam Panel System and accessories as required in accordance with manufacturer’s specifications and details.

B.	All sheet metal panel products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

# Products

2.01 Manufacturer

CopperCraft, Inc.

404 East Dallas Road

Grapevine, TX  76051

1-800-486-2723

2.02 Materials

- Copper roof panels to be 99.9% pure copper, CDA 110, ASTM B370 cold rolled temper, weighing not less than 16 ounces per square foot.

- Sheet copper for related flashing, edge strips and cladding shall be 16 oz. (.0216”) minimum.

- Concealed cleats: 16oz copper or 26ga stainless steel.

- All fasteners in contact with panels or cleats to be series 300 stainless steel.

- Solder: ASTM B32, composition 50% pig lead and 50% block tin.

- Flux: Rosin flux or muriatic acid neutralized with zinc.

- Underlayment: Flexible self-adhering rubberized asphalt membrane designed for use under architectural metal roof surfaces.

- Approved Manufacturers

- Miradri WIP 300HT

- Slip sheet: Rosin sized building paper, weighing approximately 6 lbs. Per 100 square feet.

- Sealant: ASTM C920, a one component silicone based material, movement capability +/- 50%. Color as selected by Architect.

- Approved manufacturers

- Dow Corning; 795

b.  General Electric; GeSil N

# Execution

3.01 Inspection

All surfaces to which metal panels are to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

- Install metal roofing work using skilled craftsman, in strict accordance to manufacturer’s details. Installer shall have a minimum of 5 years experience in the installation of metal roofing systems of similar design and content.

- Install the work in accordance with details shown on approved shop drawings. Details shown on drawings shall be considered typical and apply for similar features where not particularly detailed.

- Incorporate adequate and approved provision in the work to compensate for thermal expansion and contraction.

- Soldering: Perform slowly with well heated coppers and thoroughly heat the seam and sweat the solder through its full width.

- Execute seams in the direction of the flow.

F.	All sheet metal work shall conform to standards set forth in the following publications.

- Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual