CopperCraft, Inc.

Spire/Finial Specifications

# General

  - Description of work

- Furnish and install complete CopperCraft Custom/Standard Spires/Finials (with attachment points for Lightning Protection System) and other accessories as required in accordance with CopperCraft specifications and plans and details.

B.	All sheet metal products shall be manufactured by CopperCraft in sizes, styles and materials as indicated below and shown on drawings.

# Products

2.01 Manufacturer

CopperCraft, Inc.

4995 Keller Haslet Road

Keller, Texas 76248

1-800-486-2723

  - Materials

A.	Copper: 99.9% pure copper, CDA 110, ASTM Specification B370, cold rolled temper, weighing not less than 16oz per square foot.

B.	Leadcoated Copper: ASTM Specification B101 (Type 1), Class A, weighing not less than 16oz per square foot.

C.	Paint Grip: Mill phosphatized G-90 Galvanized 26ga minimum.

- Electrolytic High Grade Zinc: 99.995% pure with alloying additives of copper and titanium, .7mm minimum.

- Mill Finish Aluminum: Alloy 3003-H14, Lock forming quality (LFQ), ASTM B209, .032 minimum.

- If indicated on drawings, have Spire/Finial coated with a post applied Kynar 500 paint system (selected from the manufacturers standard colors) (in a custom color as selected), by the Architect.

# Execution

3.01 Inspection

All surfaces to which sheet metal is to be applied shall be smooth, sound, clean, dry, and free from defects that might affect the application.

3.02 Installation

A.	All sheet metal work shall conform to standards set forth in the following publications.

- Sheet Metal and Air Conditioning Contractors National Association, Inc. (SMACNA) Architectural Sheet Metal Manual

- Copper Development Association (C.D.A.) Copper Brass Bronze Design Handbook

- Revere Copper Products, Inc,; Copper and Common Sense

B.	Install Spire/Finial with brackets provided or as directed by the Architect.